**PC3710 –***Thermally Broken Perimeter Channel*

**Product Specifications**

**Specification Details:**

* Division:
	+ 08 88 00: Special Function Glazing
* Materials:
	+ Channel: 6063-T5 Aluminum
	+ Interior/Backer Gasket: 60 Durometer EPDM with Cord
	+ Exterior/Wedge Gasket: 70 Durometer EPDM
	+ Setting Block: Acetal delrin
* Mount Type: Vertical mount on top of or base of OR flush with finished surfaces
* Mount Structure: Concrete, steel or wood (by others)
* Infill: Glass Thickness of 25.5 to 37.5mm [1" to 1 1/2"]
* Finish Options: Mill, anodized, painted, powder-coated, and/or brushed stainless steel cladding
* LEED Standards:
	+ Aluminum (primary material) - 25% pre-/90% post- consumer recycled content by weightCompliances/Standard: Project specific
* Warranty: 2-year limited warranty\* (can be project specific)