**ST503TH6S25013 -***Adjustable Stand-off - Tapered Face*

**Product Specifications**

**Specification Summary:**Adjustable Stand-Off – Taper Face Fitting: Provide Type 316 finished stainless steel with black gaskets and ferrule bushing able to accommodate 12 mm to 21.5 mm glass thickness and adjustable stand-off thickness between 48 mm and 58 mm. Loading Capacity: Lateral load 4kN, Tensile load 4kN, Compressive load 4kN. Permitted Product: “Model ST503TM6S” by Stella; www.stellaglasshardware.com.

**Specification Details:**

* Division:
	+ 05 73 13: Glazed Decorative Metal Railings
	+ 08 88 00: Special Function Glazing
* Materials:
	+ Adjustability: +/- 6mm [1/4"] in/out adjustability
	+ Steel: Grade 316 stainless steel
	+ Finish: No. 4, 320 grit
	+ Gaskets: Material based on high-quality aramid fibers and special functional fillers bonded with NBR, sulfur-free, solvent-free.
* Ferrule Bushing: Acetal delrin
* Mount Type: Vertical mount on top of or below
* Mount Structure: Steel - max steel thickness 16mm [5/8"]
* Glass Thickness: 12 to 21.5 mm [1/2" to 7/8"]
* Loading Capability: Lateral load 4kN, Tensile load 4kN, Compressive load 4kN
* LEED Standards:
	+ Stainless Steel (primary material) - >45% pre-/95% post- consumer recycled content by weight
* Compliances/Standard: Project specific
* Warranty: 2-year limited warranty\* (can be project specific)